PRODUCT  SPECIFICATION

1.PRODUCT  CODE    ATC37032

2. DESCRIPTION          3 Core 7/.32  (0.56sqmm) .P.C.W.  V90  PVC  insulated.

5V90  P.V.C.  sheathed  trailer  cable.

60 Volt . Not for Mains  connection.

3. CONSTRUCTION

3.1  CONDUCTOR :  7  strands  of  0.32mm  Annealed  Copper  to

AS1125  drawn  from  Class  102  copper  to

AS1574.

Max.  D.C. resistance  at  20C  : 33.0 ohms / km

3.2  INSULATION :    Coloured  V90  PVC  to  AS3808.

Nominal  Diameter  :  1.8  mm

Nom.  Wall  Thickness:   0.4  mm

3.3  LAY  UP                3  Cores  laid  up

1. White    2. Yellow    3.Green

3.4  SHEATH               Coloured  P.V.C.  type 5V90  to  AS3808.

Nominal  Diameter :  4.9  mm

Nom.  Wall  Thickness :   0.6  mm