PRODUCT  SPECIFICATION

1.PRODUCT  CODE    HML32402

2. DESCRIPTION          3 Core 24/.20  (.75 mm sq  ,7.5amp) .P.C.W.  V75  PVC  insulated.

4V75  P.V.C.  sheathed.   Cable .

Generally 250/440 Volt .

3. CONSTRUCTION

3.1  CONDUCTOR :  24  strands  of  0.20 mm  Annealed  Copper  to

AS1125  drawn  from  Class  110A  copper  to

AS1574.

Max.  D.C. resistance  at  20C  : 26.07 ohms / klm

3.2  INSULATION :    Coloured  V75  PVC  to  AS3808 .

Nominal  Diameter  :  2.3  mm

Nom.  Wall  Thickness:   0.6  mm

3.3  LAY  UP                3  Cores  laid  up .

1. Red   2. Black.  3. White

3.4  SHEATH               Coloured  P.V.C.  type 4V75  to  AS3808.

Nominal  Diameter :  6.65  mm

Nom.  Wall  Thickness :   0.8  mm