PRODUCT  SPECIFICATION

1.PRODUCT  CODE    MWS22402

2. DESCRIPTION         2 Core  Flat  Twin  Sheathed  24/.2  ( 0.75 mm sq) .T.A.C.W.                              			            75c  insulated  &  Sheathed. Extra Low  Voltage .

Not  for  Mains GPO Connection.

3. CONSTRUCTION

3.1  CONDUCTOR :  24  strands  of  0.2 mm  Tinned  Annealed  Copper  to

AS1125  drawn  from  Class  110A  copper  to

AS1574.

Max.  D.C. resistance  at  20C  :  26.7 ohms / klm

3.2  INSULATION :    Coloured  V75  P.V.C. to  AS3808.

Nominal  Diameter  :  2.4mm

Nom.  Wall  Thickness:  0.6mm

3.3  CORE  COLOURS

1. White     2. Black

Laid  parallel.

3.4  SHEATH         :    Coloured  4V75  to  AS3808

Flat  configuration

Nominal  Dimensions  :4.2x6.4  mm

Nom.  Wall  Thickness  : 0.76  mm