PRODUCT  SPECIFICATION

1.PRODUCT  CODE    TMP13705

2. DESCRIPTION          13  Core 7/.5  (1.5sqmm) .P.C.W.  UV stabilised polypropylene insulated.

Score and snap UV stabilised  TYFLO MP.  sheathed  irrigation  cable.

Extra Low Voltage . Not for Mains  connection.

3. CONSTRUCTION

3.1  CONDUCTOR :  7  strands  of  0.5mm  Annealed  Copper  to

AS1125  drawn  from  Class  102  copper  to

AS1574.

Max.  D.C. resistance  at  20C  : 13.6  ohms / km

3.2  INSULATION :    Coloured  UV stabilised polypropylene

Nominal  Diameter  :  2.35  mm

Nom.  Wall  Thickness:   0.4   mm

3.3  LAY  UP               13  Cores  twisted .

1.  Black   2  Red   3. White  4. Blue  5. Green

6. Brown  7. Yellow  8. Pink  9. Grey  10. Violet

11. Beige  12. Light Green  13. Orange

3.4  SHEATH               Score and snap UV stabilised  TYFLO MP.

Nominal  Diameter :  11.6  mm

Nom.  Wall  Thickness :     0.7  mm