PRODUCT  SPECIFICATION

1.PRODUCT  CODE    TMP37043

2. DESCRIPTION          3  Core 7/.43  (1.0sqmm) .P.C.W.  UV stabilised polypropylene insulated.

Score and snap UV stabilised  TYFLO MP sheathed irrigation  cable.

Extra Low Voltage . Not for Mains  connection.

3. CONSTRUCTION

3.1  CONDUCTOR :  7  strands  of  0.43mm  Annealed  Copper  to

AS1125  drawn  from  Class  102  copper  to

AS1574.

Max.  D.C. resistance  at  20C  : 21.2 ohms / km

3.2  INSULATION :    Coloured  UV stabilised polypropylene

Nominal  Diameter  :  2.15  mm

Nom.  Wall  Thickness:   0.4   mm

3.3  LAY  UP               3  Cores  twisted .

1.  Black   2  Red   3. White

3.4  SHEATH               Score and snap UV stabilised  TYFLO MP.

Nominal  Diameter :   5.8  mm

Nom.  Wall  Thickness :   0.6  mm