PRODUCT  SPECIFICATION

1.PRODUCT  CODE    WMW37085

2. DESCRIPTION          3  Core 7/.85  ( 4 sqmm) .P.C.W.  UV stabilised polypropylene insulated.

4V75  P.V.C.  sheathed . TYFLO irrigation  cable.

Extra Low Voltage . Not for Mains  connection.

3. CONSTRUCTION

3.1  CONDUCTOR :  7  strands  of  0.67mm  Annealed  Copper  to

AS1125  drawn  from  Class  102  copper  to

AS1574.

Max.  D.C. resistance  at  20C  : 4.6  ohms / km

3.2  INSULATION :    Coloured  UV stabilised polypropylene

Nominal  Diameter  :  3.8  mm

Nom.  Wall  Thickness:   0.6   mm

3.3  LAY  UP               3  Cores  twisted .

1.  Black   2  Red   3. White

3.4  SHEATH               Coloured  P.V.C.  type 4V75  to  AS3808.

Nominal  Diameter :    9.9  mm

Nom.  Wall  Thickness :     0.7  mm