**PRODUCT SPECIFICATION**

****

**1. PRODUCT CODE:** ATC52603

**2. DESCRIPTION 5 Core 23/.32 (1.84mm2).**

**Plain Copper Wire**

**V90 P.V.C. Insulated and 5V90 P.V.C. Sheathed Trailer cable.**

**Extra Low Voltage. Not for Mains connection.**

**RoHS compliant P.V.C.**

**Oxygen Free copper.**

**3. CONSTRUCTION**

**3.1 CONDUCTOR:** 23 strands of 0.32 mm nom. Annealed Copper to AS/NZS1125

drawn from Class 102 copper to AS/NZS1574.

Max. D.C. resistance at 20C: 10.3 ohms / km

**3.2 INSULATION:** Coloured V90 P.V.C. to AS/NZS3808.

Nominal Diameter: 2.6 mm

Nominal Wall Thickness: 0.4 mm

**3.3 LAY UP:**  5 Cores laid up.

1. Brown

2. Red

3. Green

4. White

5. Yellow

**3.4 SHEATH:** Coloured P.V.C. type 5V90 to AS/NZS3808.

Nominal Diameter: 8.2 mm

Nominal Wall Thickness: 0.6 mm

**TYPICAL ROPY TRAILER CABLE FINISH**

 