PRODUCT  SPECIFICATION

1.PRODUCT  CODE    WSE17170

2. DESCRIPTION          	7/1.70  ( 16 mmsq) Plain  annealed  copper

UV stabilised  polypropylene  insulated

Extra  Low  Voltage  Irrigation  Cable.

3.1  CONDUCTOR :   7  strands  of  1.70 mm  nom.  Plain  Annealed  Copper  to

AS1125 drawn  from  Class  102  copper  to  AS1574.

Max.  D.C. resistance  at  20C  : 1.15 ohms / km

3.2  INSULATION    Coloured  UV STABILISED Polypropylene				 					Nominal  Diameter :      7.1   mm

Nominal  Wall  Thickness :      0.8   mm